## Slide 1
Dark field and transmission in the Compton regime
Matteo Abis, Pablo Villanueva Perez, Zhentian Wang, Marco Stampanoni
Institute for Biomedical Engineering, University and ETH Zürich, Zürich, Switzerland
Swiss Light Source, Paul Scherrer Institut, Villigen, Switzerland

## Slide 2
What is the Compton regime?
Energy > 40-50 keV for biomedical applications
2
Matteo Abis – XNPIG2015

## Slide 3
Signals from phase stepping curves
Moduli of the first two Fourier coefficients
Transmission
Dark field
Ratio
3
Matteo Abis – XNPIG2015

## Slide 4
The ratio in literature below 40 kVp
Independent of thickness
Depends on atomic number
Depends on microstructure size
Wang and Stampanoni, Quantitative x-ray radiography using grating interferometry: a feasibility study, 2013
Scherer et al., Non-invasive Differentiation of Kidney Stone Types using X-ray Dark-Field Radiography, 2015
4
Matteo Abis – XNPIG2015

## Slide 5
Experiment at 160 kVp
5
Matteo Abis – XNPIG2015

## Slide 6
Experiment at 160 kVp
6
Matteo Abis – XNPIG2015
R independent of thickness
R depends on atomic number
R depends on microstructures

## Slide 7
No Z information
Given by photoelectric absorption
Irrelevant above 50 keV
7
Matteo Abis – XNPIG2015

## Slide 8
Microstructures
Lynch et al. 2011, synchrotron experiment, analytical description
8
Matteo Abis – XNPIG2015

## Slide 9
Microstructures on polychromatic sources
Compute the contribution as in Lynch et al for each energy
Sum over spectral weights
Our model, with 2 parameters and :
9
Matteo Abis – XNPIG2015

## Slide 10
Spectral weights
source visibility detector efficiency sample abs.
Simulated source (SpekCalc)
Detector efficiency and sample abs. from NIST coefficients
Visibility as a function of energy from Thüring et al., Performance and optimization of X-ray grating interferometry, 2014
10
Matteo Abis – XNPIG2015

## Slide 11
Silica microspheres 0.16 to 7.75 μm
Fit the two parameters and :
Samples with two different thicknesses
11
Matteo Abis – XNPIG2015
t (mm) |  | C
12 | 2.73(12) | 5(1)
45 | 2.31(15) | 11(2)
t (mm) |  | C
12 | 2.73(12) | 5(1)
45 | 2.31(15) | 11(2)

## Slide 12
Conclusions
Good model for dark field above 50 keV on polychromatic sources
Effective Z information is lost
Fully complementary information on microstructures can be retrieved with
means that the phase signal is very difficult to recover
12
Matteo Abis – XNPIG2015

## Slide 13
Acknowledgements
13
TOMCAT Team